HYDROPRUF WP300

Anti-crack Integral General Waterproofing Admixture for Concrete and Plaster

Product Description:

Hydropruf  WP300  is  a  specially  formulated  Liquid  anti-crack,  integral,  general  waterproofing admixture  which  reduces  the  transmission  of  water  through  concrete,  mortar  and  screed.  It is suitable for use in all concrete, mortar or screed. Typical  applications areas  include, wall plasters, Foundation, piles,  water  retaining  structures, manholes, sewage treatment plants, swimming pool,

and septic tanks.

Advantages:

	Reduces the permeability of the concrete, plaster and screed, thereby increasing building durability.

	Unlike coatings, HYDROPRUF WP300 when added to plaster or concrete during mixing becomes an integral part of the concrete and plaster; hence, waterproofing protection is still maintained even if surface damage occurs.

    It helps to increase the compressive strength of concrete

    Protects reinforcement bars against ASR attack and corrosion

	Helps to reduce shrinkage crack development in concrete and Plaster especially in hot weather.

    Increases the overall workability of concrete during placement

Standard Compliance and Specification:

    HYDROPRUF WP 300 meets the water absorption requirements of the European Standard

BSEN934-2.

Typical Application Areas:

HYDROPRUF WP300 can be used for the waterproofing of all types of concrete, plaster and screed. such as:

    Foundation

    Swimming pool

    Wall plaster and Screeding

    Septic tank

    Water retaining structures

    As a complimentary protection in the Screeding of terraces, Balconies and Roof Gutters.

    All concrete, Mortar and Screed requiring waterproofing.

Dosage:

The recommended dosage for HYDROPRUF WP300 is 0.5% to 1% of cement content. However, optimum dosage to meet specific requirements should always be determined by trials using the admixture on site.

Limitation:

HYDROPRUF WP 300 Is not a replacement for good concrete practice. Please note that no amount of waterproofing admixture can replace and make up for poor quality concrete. As a minimum requirement Armorsil recommends a minimum of 300 kg of cement per cubic of concrete.

Technical Information:

Appearance                     : Turbid Solution

Specific Gravity              : Typically 1.05 at 20°C

Chloride Content           : Nil to BS 5075

Water permeability test: 2645: 2003 Passed

Packaging:

P300  is packed in 20KG  and 5kg kegs

Health and Safety Precautions:

HYDROPRUF WP300 should not be swallowed or allowed to come into contact with skin and eyes. Please use gloves and protective goggles

Shelf Life:

HYDROPRUF WP300 has a shelf life of 12 months.

Limited Warranty

All recommendations, statements and technical data herein are based on tests we believe to be reliable and correct, but accur acy and completeness of said tests are not guaranteed and are not to be construed as a warranty either e x p r e s s e d or implied. User shall rely on his or her own information and tests to determine suitability of the product for the intended use and user assumes all risk and liability resulting from his or her use of the product. Nothing contained in any supplied materials relieves the user of the obligation to read and follow the warnings and instruction for each product as set forth in the current Technical Data Sheet, product label and Safety Data Sheet prior to product use away. Armorsil Manufacturing supplies products that comply with the properties shown on the current datasheets. In the unlikely event that products supplied are proved not to comply with these properties, then we will replace the non-compliant product or refund the purchase price. Armorsil Manufacturing does not warrant or guarantee the installation of the products as it does not have control over the installation or end use of the products. Any suspected defects must be reported to Armorsil Manufacturing in writing within seven working days of being detected.

Armorsil Manufacturing. Makes no warranty as to merchantability or fitness for a particular purpose and this warranty is in lieu of all other warranties express or implied. Neither seller nor Armorsil Manufacturing shall be liable to the buyer or any third person for any injury, loss or damages of any sort including remote or consequential damages, down time, or delay directly or indirectly resulting from use of or inability to use the product. . The information contained in the latest data sheet supersedes all previously published editions. Visits to site by Armorsil personnel do not constitute supervisory responsibility. Armorsil rese rves the right to alter the information contained in this datasheet without prior notice

ARMORSIL MANUFACTURING INCORPORATION

- 4636 Chestnut Street, Philadelphia, Pennsylvania 19139 . Tel : +1 209 813 246     +1 415 670 9521

- www.armorsil.com,    info@armorsil.com, sales@armorsil.com

## PROVIDING ARMOR FOR BUILDING STRUCTURES

# Text boxes

General Waterproofing Admixture